**Schedule 2**

Uses IS 2 – no IS 0 – and actually requires examination for smoulder as well as open flame ignition.

The cover in every case is the standard FR Trevira CS fabric.

Morgan says that thermoplastic covers do not or some qualified case in between exhibit smoulder.

Schedule 2 covers all non-foam materials used in mattresses unless they are subjected to a final composite rig test = BS EN 597.

No filling is tested with anything other than open flame and though a smoulder assessment is made there is no condition that assesses smoulder conditions.

The REGS say:

    (3)  A cushion may include filling material which does not pass the ignitability test specified in Part I or Part II (or both such parts) of Schedule 2 to these Regulations if the cushion has a primary cover and, with that cover, passes the ignitability test in Part III of that Schedule.  
  
    (4)  A pillow may include filling material which does not pass the ignitability test specified in Part I or Part II (or both such parts) of Schedule 2 to these Regulations if the pillow, when tested with its primary cover, passes the ignitability test in Part III of that Schedule.

**Loose fillings**  
    **7.**    No person shall supply any filling material which fails the relevant ignitability test, or which contains foam in crumb form which may not be included in furniture by virtue of regulation 6(2) above, in any case where he knows or has reasonable cause to believe that the material will be used-

 (a) for filling a cushion or a pillow; or

 (b) for the purpose of upholstering or re-upholstering furniture.